PbLi Procurement Issue

Taesuk Oh

Material composition and production:

- Pb-17Li eutectic contains ~99.4 wt% Pb and ~0.6 wt% Li.

- The alloy is produced through conventional metallurgical melting and mixing of lead and lithium under inert atmosphere.

- Because the lithium fraction is very small, large-scale alloy fabrication is not expected to be technically complex once lithium feedstock is available.

- The primary material supply issue discussed in fusion literature is access to enriched lithium (especially Li-6) rather than the production of the Pb-Li alloy itself.

Existing experimental PbLi facilities

- Multiple research laboratories already operate flowing Pb-17Li loops for corrosion, MHD, and tritium technology studies.

- These facilities demonstrate that PbLi circulation and handling technologies are experimentally established.

[1] KIT – PICOLO loop (Germany)

- Purpose: corrosion testing of structural steels in flowing Pb-17Li.

- Reported operating conditions include ~480 °C flowing Pb-17Li for long-term exposure tests (up to ~10,000 h).

- Inventory reported in technical documentation:

  - ~15 L Pb-15.7Li in the loop, corresponding to roughly ~140 kg of PbLi.

[2] UCLA PbLi MHD facility (United States)

- Purpose: magnetohydrodynamic flow and liquid-metal blanket technology experiments.

- Reported inventory:

  - ~200 kg PbLi circulating in the experimental loop.

[3] DRAGON-V PbLi facility (China)

- Engineering-scale test facility for liquid-metal blanket technology.

- Reported inventory:

  - ~20 tons PbLi, significantly larger than typical laboratory loops.

Implications for PbLi supply

- Experimental systems ranging from O(10² kg) to O(10¹ t) inventories have already been constructed and operated.

- This indicates that PbLi alloy preparation, storage, and circulation are engineering-feasible technologies.

- Given that the alloy is overwhelmingly composed of lead, and global lead production is large, Pb availability is unlikely to represent a limiting factor.

- Consequently, from a supply-chain perspective, the more credible constraint for Pb-Li blankets is lithium isotope enrichment capacity (Li-6) rather than Pb-Li alloy fabrication itself.